## Slide 1: Light Flexible Bulletproof Vest
Paola Briceno Aurelio Matthew Leal Teodor Nonov
Faculty Advisor: Dr. Shirazi & Dr. Haider
Course Advisor: Dr. Sarkar

## Slide 2: OUTLINE
Overview
Elevator Speech
Background Research
Competitive Products
Needs and Wants
Problem Definition
Objective
QDF
Final Design
Functional Decomposition
Abaqus Model
Design Model
Manufacturing
Bill of Materials
Manufacturing Process
Retail Price
Test Details
Testing Goals
Testing Procedures
Test Results
Tests 1-4
Results and Discussion
Top Design
Best Practices
Lessons Learned
Timeline
Summary
Future Recommendations
References

## Slide 3: OVERVIEW

## Slide 4: BODY ARMOR BACKGROUND INFO
Total Industry : $734 Million
  79 Businesses
  4 Companies Own 52%
Body Armor Customer Basis
Chart: 
| Military | Law Enforcement | Other Commercial
Body Armor Customer Basis | 0.72 | 0.142 | 0.138

## Slide 5: BODY ARMOR CLASSIFICATIONS
Main Focus For Senior Design Project

## Slide 6: COMPETITIVE PRODUCTS
Company | Type | Weight | Cost | Materials Use | Contact Information
safeguard clothing | NIJ Level IIIA Ballistic Protection, NIJ Level II edged blade protection NIJ Level II Spike Protection | 5.5lbs | $800 | CoolIMAX lining, poly-cotton, DuPont Kevlar. | Safeguard Clothing Phone# :888 958 0168
GH Armor Systems GH PRO | NIJ LEVEL IIIA Ballistic Protection | _ | $435 | Polycotton carrier lines with akwadyne coolmesh material for comfort, water resistant ballistic panel cover. | 1479 Gillespie Street, Suite 303.Rock Island, Illinois 61201 Phone: 563.823.6652
 | NIJ LEVEL IIIA Ballistic Protection | _ | $705 | designed with 100% Aramid(Kevlar), Polycotton carrier lined with Aquadyne Coolmesh material | 
Diamondback Tactial | NIJ Level IIIa Ballistic Protection | - | - | Hybrid construction of core felt and UD laminates (Honeywell Spectra shield and gold shield materials) | Diamondback Tactical,LLLP 207 Oakland Rd. Spindale, NC 28160 1-800-882-7667
United Shield International | NIJ Level IIIa Ballistic Protection | - | - | Aramid, polyethylene, and ceramic materials technology, other ballistics components. | 1606 Barlow St Unit 1 Traverse City, MI 49686 USA Phone: +1 231 933 1179
US Armor | NIJ Level IIIa Ballistic Protection | - | - | Honeywell Spectra shield and gold shield materials, Du Pont Kevlar. | 10715 Bloomfield Avenue Santa Fe Springs, CA PH: 800-443-9798

## Slide 7
NEEDS
Comfort
Lighter Weight
Minimal Movement Constraints
Decrease Trauma Levels
NIJ Level IIIA Threat Compliance
WANTS
Appliance/Device Storage Pockets
Color Styling and Patterning
Concealability
Increased Permeability

## Slide 8
GOALS
Comfortable for Wearer
Lighter Weight
Minimal to No Movement Constraints
Decrease Trauma Levels
OBJECTIVES
Below 6lbs Weight
Vest Retail AT $600
Comfortable for Wearer
Pass NIJ Level IIIA Requirements
Attention/Funding

## Slide 9: CONSTRAINTS
Time
  3 months R&D
  4 months prototype creation
Available funding
  $300 USD
Lack of Information for Main Corporations
  Vest Materials and Configuration Properties
Lack of Required Materials
  Can’t Make a Complete Vest

## Slide 10: QUALITY FUNCTION DEPLOYMENT

## Slide 11: FINAL DESIGN

## Slide 12: FUNCTIONAL DECOMPOSITION
Chart: 
| 1st Qtr | 2nd Qtr | 3rd Qtr
Sales | 33.3 | 33.3 | 33.3
Material

## Slide 13: BULLET IMPACT SIMULATION
Assumed Symmetry for Model
  Bullet impacting center of protective layers
  9” x 9” layers (1/4 of chest protective layer size)
  1/4 of .357 SIG flat nose full metal jacket modeled
Bullet to impact bottom right of protective layers exactly in corner (symmetry)
BC’s are being assigned symmetry at bottom and right side of bullet/layers
Other sides layering set with only rotation limitations outward

## Slide 14: MESH VIEW OF MODEL

## Slide 15: PROTECTIVE LAYERING
12 Kevlar and 12 Spectra
Kevlar-Green
Spectra-Grey
Kevlar .0118 meters
Spectra .006 meters
Thickness difference implies more Kevlar

## Slide 16: .357 SIG FLAT NOSE FMJ
.354” Diameter
.4” Length
.003” Thick Cu Jacket
Lead- Red
Copper- Blue-green

## Slide 17: ASSEMBLY AND BCs
Assembled with Bullet Lined up at Bottom Right of Layering for Symmetry Assimilation
BCs for bottom and right sides of the bullet and layering for symmetry
Other layer BCs set with rotational condition preventing it from rotating out
.357 velocity set at -448m/s in Z

## Slide 18: ABAQUS RESULTS
Numerical Results were Unable to be Obtained Due to Issues Obtaining a Program that Could Run the Model.
This Led to a Need to Come Up with Useful Physical Testing Method
Future Teams will be Able to Use the Program to Test and Improve Designs

## Slide 19: DESIGN MODEL
18 in
16 in

## Slide 20: MANUFACTURING

## Slide 21: Bill of Materials
Product | Vendor | Quote
Kevlar KM2 | Infinity Composites Inc. | $95.02
Ballistic Spectra Fabric | Composite Envisions LLC. | $154.10
Kevlar Thread | The Thread Exchange | $21.37
Bungee Cord | Lowes | $20.52
.44 Mag Bullets | Remington | $50
Sand Bags | Lowes | $12
Lumber for Frame | Lowes | $20
Total: | - | $373.01

## Slide 22: MANUFACTURING PROCESS
Cut Sheets of Kevlar KM2 and Spectra 1000 into the vest pocket shapes.
Place Fibers into chosen configuration.
Sew configuration with industrial machine (15.24 cm sewn sections to hold layers together).
Place the protective layers between nylon and seal it.

## Slide 23: RETAIL PRICE
# Vests Produced: 4901
Production Cost: $355.09
Distributor Cost: $461.54
Profit: $106.45
Retail Price: $600
Target QFD Price: $600
Competitive Prices: $600-$800
Market Size: $3 Million

## Slide 24: TEST DETAILS

## Slide 25: TESTING GOALS
Test 1-
Analyze the Effect of Ply Orientation
Test 2-
Test Different Combinations
Analyze Kevlar and Spectra Behavior When Impacted
Test 3-
Investigate Aerial Weight and its Effect on Fabric Strength
Test 4-
Compare our Configuration with Real Life Vest (Exact Same Aerial Weight)

## Slide 26: TESTING PROCEDURE
Cut 4in x 4in Sheets of Kevlar KM2 and Spectra 1000
Use All Kevlar Specimens to Create 3-24 Layer Sample Pads in Varying Ply Orientations
    0 to 45 Degree Ply Alternating
    0 to 45 Degree Ply
    0 Degree Un-oriented

## Slide 27
Hang Configuration using Bungee Cords Around Sand Bags
Use .357 Mag to Shoot the Protective Pads from Distance of 1 Foot
Analyze each Test Specimen to Determine Best Ply Orientation.

## Slide 28: UPDATED TESTING PROCEDURES
Constrain Pads Clamping between Wooden Frames Using 4 Bolts through Frame (3ft-lb Torque Per Bolt)
Place Wood Backing With .625in Clay Barrier Behind Test Coupon
2.5”x2.5”
.625”

## Slide 29: UPDATED TESTING PROCEDURE
Test 3 Configurations with 24 Layers & Vest Pad
    12 Kevlar and 12 Spectra
    24 Kevlar
    24 Spectra
Match Kevlar and Spectra Aerial Weights with Varying Configurations
  20 Kevlar 10 Spectra
  16 Kevlar 20 Spectra
  12 Kevlar 30 Spectra
Match Aerial Weight of Kevlar and Spectra Top Pads to Honeywell IIIa Gold Flex
  25 Kevlar
  20 Kevlar 13 Spectra
  Honeywell IIIa Gold Flex

## Slide 30: TESTING RESULTS

## Slide 31: TEST 1 SETUP
Shooting Distance: 1 Foot
Bullet Used: .357 Magnum SJHP (125grain)
Restrains: None (Freely Hanging)

## Slide 32: VIDEO OF TEST 1 IMPACT

## Slide 33: TEST 1- SAMPLES
Sample 1
24 Layers Kevlar
No Variation in Ply Orientation
Sample 2
24 Layers Kevlar
0 to 45 Degree Ply Alternating Every Other
Sample 3
24 Layers Kevlar
0 to 45 Degree Ply Alternating

## Slide 34: TEST 1 VISUAL RESULTS
Back Front

## Slide 35: QUANTITATIVE RESULTS
Chart: Bump Height vs. Layering
| No Variation | 0 To 45 Alternating Every other | 0 To 45 Ply Orientation
 | 0.994 | 0.994 | 0.528
Chart: Layers Penetrated vs. Layering
| No Variation | 0 To 45 Alternating Every other | 0 To 45 Ply Orientation
 | 6 | 10 | 8
Chart: Bump Area vs. Layering
| No Variation | 0 To 45 Alternating Every other | 0 To 45 Ply Orientation
 | 0.25 | 0.375 | 0.375
INCONCLUSILVE/ UNRELIABE
WHY..
Sand Absorbed much of impact due to allowed motion of pad since they were unrestrained
Single Tests conducted and some of results could be outlying values on bell curve (not enough testing)
Video results in hint to need for new testing method

## Slide 36: TESTS 2-4 SETUP
Shooting Distance: 1 Foot
Bullet Used: .357 Magnum SJHP (125grain)
Restraints: Wooden Frame with Clay Backing (3 ft-lb per bolt)

## Slide 37: TEST 2- SAMPLES
Sample 1
24 Layers Kevlar
Sample 2
24 Layers Spectra
Sample 3
12 Layers Kevlar
12 Layers Spectra

## Slide 38: TEST 2 VISUAL RESULTS
24 Layers Kevlar
24 Layers Spectra
12 Kevlar, 12 Spectra

## Slide 39: QUANTITATIVE RESULTS
 | 24 Kevlar | 24 Spectra | 12K, 12S
Layers Penetrated | 6 | 24 | 24
Volume Affected | .0089in^3 | - | -
Back Indention (Height, Area) | .469in and 1.03in^2 | - | -

## Slide 40: TEST 2 OUTCOMES
24 Kevlar Sample Stopped the Bullet
24 Spectra and 12K12S Pad Were Compromised by Bullet Impact
24 Spectra had Least Energy Dissipation Based on Hole Left in Wood
24 Kevlar Sample Most Successful in Decreasing Bullet Energy and Trauma

## Slide 41: FURTHER TESTING
Investigate Aerial Weight and its effect on Fabric Strength
Create a Kevlar and Spectra Pad using Aerial Weight Matching System for Layers
Investigate Laminating Layers

## Slide 42: TEST 3 – SAMPLES
Sample 1
20 Kevlar, 10 Spectra
Sample 2
16 Kevlar, 20 Spectra
Sample 3
12 Kevlar, 30 Spectra

## Slide 43: TEST 3 VISUAL RESULTS
12 Kevlar, 25 Spectra
20 Kevlar, 10 Spectra
16 Kevlar, 20 Spectra

## Slide 44: QAUNTITATIVE RESULTS
Chart: Bump Height vs. Layering
| 24K | 20K 10S | 12K 30S | 25K | 20K 13S | GoldFlex IIIa
Bump Height | 0.469 | 0.475 | 0.582
Chart: Layers Penetrated vs. Layering
| 24K | 20K 10S | 12K 30S | 25K | 20K 13S | GoldFlex IIIa
Layers Penetrated | 6 | 11 | 10
Chart: Bump Area vs. Layering
| 24K | 20K 10S | 12K 30S
Bump Area | 1.03 | 0.97 | 0.86
16 K,20 S Unreliable

## Slide 45: TEST 3 OUTCOMES
All 3 Different Samples Stopped the Bullet.
Confirm Aerial Weight Affects Strength
12 Kevlar-25 Spectra and 20 Kevlar-10 Spectra Successful
16Kevlar-20Spectra Data Unreliable Due to Knot in Wood’s Affect on Impact

## Slide 46: FURTHER TESTING
Test Commercial Product with Goldflex IIIa Protective Layering
Compare Aerial Weight of Kevlar and Spectra to Commercial Product
Create all Kevlar Pad Based on Comparative Aerial Weight
Create Kevlar-Spectra Layering Based on Comparative Aerial Weights

## Slide 47: TEST 4 – SAMPLES
Sample 1
Commercial Product
Sample 2
25 Kevlar
Sample 3
20 Kevlar, 13 Spectra

## Slide 48: VISUAL RESULTS
20 Kevlar, 13 Spectra
25 Kevlar
Commercial Product

## Slide 49: QUANTITATIVE RESULTS
Chart: Bump Height vs. Layering
| 25K | 20K 13S | GoldFlex IIIa
Bump Height | 0.46 | 0.453 | 0.25
Chart: Layers Penetrated vs. Layering
| 25K | 20K 13S | GoldFlex IIIa
Layers Penetrated | 5 | 5 | 2
Chart: Bump Area vs. Layering
| 25K | 20K 13S | GoldFlex IIIa
Bump Area | 1.33 | 2.09 | 5.85

## Slide 50: TEST 4 RESULTS
All Samples Successful in Stopping Bullet
Commercial Product with Goldflex IIIa Protective Padding Displayed Greatest Energy Dissipation of Bullet
Due to Lamination, Breathability of Goldflex IIIa Product is Less than that of Kevlar/Spectra Non Laminated Layers
Kevlar with Spectra Layering Next Best at Dissipating Bullet Energy Based on Area of Bump Bullet Left from Impact (Lower Pressure)

## Slide 51: RESULTS & DISCUSSSION

## Slide 52: TOP DESIGN
20 Kevlar, 13 Spectra
  Least Body Trauma Based on Resulting Bump Area
  Matches Weight of Commercial Product
  Increased Breathability Compared to Commercial Product due to Lack of Lamination
BACK
FRONT

## Slide 53: BEST PRACTICES
Using Smaller Sections of Material to Make Test Pad instead of Creating Multiple Vests to Test
Designing More Consistent Testing Method to Alleviate Undesired Variables
Matching Aerial Weight of Commercial Product to Our Product

## Slide 54: LESSONS LEARNED
More Time Spent On Planning and Organizing Leads to Less Time Working on the Project, Lower Costs, and Greater Efficiency
Don’t be Afraid to Ask for Advice

## Slide 55: TIMELINE

## Slide 56: GANTT CHART
 | January |  | February |  |  |  | March |  |  |  |  | April |  |  |  | May | 
Plan | 19 | 26 | 2 | 9 | 16 | 23 | 2 | 9 | 16 | 23 | 30 | 6 | 13 | 20 | 27 | 4 | 11
Technical Presentation |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Develop Ply Oriented Test Coupon |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Test Ply Oriented Coupons |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Develop Coupons with Same Number of Layers |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Test Same Laye r Count Coupons |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Develop Coupons w/Alternating Kevlar and Spectra |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Test Coupons with Alternating Kevlar and Spectra |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Develop Coupons Matching Aerial Weight of Goldflex II1a |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Test Matching Aerial Weight Coupons |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Run Abaqus Model |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Finish Final Report |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Final Presentation |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 57: SUMMARY
Overview
Final Design
Market Analysis/Cost
Manufacturing
Timeline

## Slide 58: FUTURE RECOMMENDATIONS
Develop Coupons Using Lamination for Kevlar KM2 and Spectra 1000 Combinations
Order Lighter Aerial Weight Kevlar and Higher Aerial Weight Spectra and Create Pads of Materials with Matching Aerial Weight Values to Find Optimal Range
Run ABAQUS Program and Investigate Varying Configurations
Add Polymer/ Polymer Nanofiber Coating to Configurations

## Slide 59: QUESTIONS
Dr. Sarkar Approved

## Slide 60: REFERENCES
Armor UP L.P. Dba." BulletProofME.com Body Armor/ Bullet Proof Vests.N.p.,n.d.Web.23 Nov.2014.
"Body Armor Manufacturing in the US: Market Research Report." Body Armor Manufacturing in the US Market Research. IBISWorld, 2014. Web. 23 Nov. 2014.
"Boron Carbide (B4C) - Properties and Information about Boron Carbide." Properties:. AZOM, n.d. Web. 10 Oct. 2014. <http://www.azom.com/properties.aspx?ArticleID=75>.
"Carbon Fiber Characteristics." Carbon Fiber Properties. N.p., n.d. Web. 10 Oct. 2014. <http://www.christinedemerchant.com/carboncharacteristics.html>.
Cheng, Ming, Weinong Chen, and Tusit Weerasooriya. "Mechanical Properties of Kevlar® KM2 Single Fiber." Journal of Engineering Materials and Technology 127.2 (2005): 197. Web.
Fact Sheet. Atlanta, Ga. (1600 Clifton Road, N.E., Atlanta 30333): ATSDR, 1990. Web
"Kevlar Bullet Proof Vests." About.com Inventors. About.com, n.d. Web. 23 Nov. 2014.
"Large Bullet Proof Body Armor Level IIIA." Rugged Earth Sports. N.p., n.d. Web. 23 Nov. 2014.
Mechanical Properties of Carbon Fibre Composite Materials, Fibre / Epoxy Resin (120°C Cure). Performance Composites, July 2009. Web. 10 Oct.
2014. <http://www.performance-composites.com/carbonfibre/mechanicalproperties_2.asp>.
Spectra Fiber 1000 High Strength Light Weight Polyethylene Fiber. Honeywell, n.d. Web. 12Oct.2014. <http%3A%2F%2Fwww.honeywell.com%2Fsites%2Fservlet%2Fcom.merx.npoint.s
ervlets.DocumentServlet%3Fdocid%3DD19CB058F-D839-EA79-85BC-E26A581EAB36>.
"United States Department of Defense." Defense.gov Contracts for Thursday, August 07, 2008. N.p.,n.d. Web. 23 Nov. 2014.

## Slide 61: APPENDIX

## Slide 62: PRODUCTION COST
 | Unit | Year
Labor Cost: Employees - 10 production, 2 engineers,1 manager | $112.22 | $550,000
Material Cost | $183.64 | $900,000
Total of Material Plus Labor (Rounded) | $316.26 | $1,550,000
Production Cost (includes 20% Overhead) | $355.09 | $1,740,000
Distributor Price (30% Profit) | $461.54 | $2,262,000
Retail Cost (30% Profit) | $600 | $2,940,600