## Slide 1: Next Generation Drywall
Faculty Advisor:Dr. Sarkar & Dr.Jones
Course Advisor: Dr. Sarkar
Daniel Quezada
Ivonne Martinez
Alexsandra Villarreal

## Slide 2: Next Generation Drywall
Faculty Advisor:Dr. Sarkar & Dr.Jones
Course Advisor: Dr. Sarkar
Daniel Quezada
Ivonne Martinez
Alexsandra Villarreal

## Slide 3: Outline
Problem Formulation
  Elevator Speech
  Background Research
  Competitive Products
  Needs & Wants
  Goals, Objectives & Constraints
  QFD
Concept Development
  Functional Decomposition
  Methodology
  Concept Generation
  Product Concept
Design Embodiment
  Engineering Analysis
  Proposed Product
  BOM
Design for Manufacturability
Manufacturing Process
Design Validation
  Test Protocols
  Safety Analysis
  Economic Analysis
Summary
References

## Slide 4: PROBLEM FORMULATION

## Slide 5: Elevator Speech
  Problem Definition
    Fire resistant drywalls are more expensive.
    Not commonly used in residential constructions.
  Impact
        Manufacture Next Generation drywall
        Affordable price with the ability to resist fire
        Better Insulation
        Better acoustic attenuation

## Slide 6: Market Research
The US produces 28% of the world's gypsum wallboard production.
American Gypsum
  Capacity: 308.6M m2/yr.
Total Capacity of 12,866M m^2/yr.
CertainTeed Gypsum
  Capacity: 500M m2/yr.
Georgia Pacific
  Capacity: 600M m2/yr.
National Gypsum
  Capacity: 830M m2/yr.
PABCO
  Capacity: 147M m2/yr.
USG
  Capacity: 835M m2/yr.
1st
2nd
3rd
4th
5th
6th

## Slide 7
MARKET RESEARCH |  |  |  |  | 
Total Market (m2/yr.) | 12,866M |  |  |  | 
Name | Location | website | Product Info | Contact Info | Production
Toughrock | Atlanta GA | www.buildgp.com | 5/8-in x 4-ft x 8-ft Fire Resistant Drywall Panel | Lowes's & Georgia Pacific Building Products | 600M m2/yr.
Gold Bond | Charlotte, N.C. | www.nationalgypsum.com | 5/8-in x 4-ft x 8-ft Fire Resistant Drywall Panel | Lowe's & National Gypsum | 830M m2/yr.
SHEETROCK | Chicago, IL | www.USG.com | 5/8 in. x 4 ft. x 8 ft. Tapered Edge Gypsum Board | Homedepot & USG | 835M m2/yr.
Continental BP | Herdon VA | www.Continental-bp.com | Fire Check 0.625-in x 4-ft x 8-ft Fire Resistant Drywall Panel | Info@continental-bp.com | 

## Slide 8
COMPETITIVE PRODUCT SUMMARY |  |  |  | 
Features | Toughrock | Gold Bond | SHEETROCK | Continental BP
Firecheck® Type X | ✔ | ✔ | ✔ | ✔
Weight (5/8" x 4' x 8') | 70.4 lb | 70.4 lb | 70.4 lb | 72.32 lb
Noncombustible gypsum core |  |  |  | ✔
Glass fibers |  |  |  | ✔
Flexibility | ✔ | ✔ | ✔ | ✔
Price | $10.97 | $10.97 | $9.14 | $10.97
GridMarX® guide marks |  | ✔ |  | 
GREENGUARD Certified |  | ✔ |  | ✔
Company | Georgia Pacific | National Gypsum | USG | Continental BP

## Slide 9: Needs & Wants

## Slide 10: Needs (Customer Requirements)
High quality product on a affordable cost of less than $12 per sheet (4’X8’)
Fire resistant
  ASTM E 119
Type-X Standard
    ASTM C1396
Better (30% more) Insulation
Better Acoustic Insulation

## Slide 11: Wants (Customer Expectations)
Lightweight product ( < 71 Lb. per sheet)
Good quality product
High performance Drywall

## Slide 12: Goals
Develop Next Generation Drywall w/Advanced Features like High Thermal Insulation, Excellent Fire Retardation, & Acoustic Attenuation
Sustainable design methodology using Recycled Glass

## Slide 13: Objectives
Increase thermal insulation by 30% using Nano particles.
Prolongation of fire retardant capacity to more than 20 min.
Maintain weight under 2.2lb/SF
Keep final product cost below $11.00

## Slide 14
Affordable Price
Type - X
Thermal Insulation
Flexibility
Fire Resistant
Light weight
Strength
Long Life Cycle
Needs
Wants
QFD

## Slide 15: CONCEPT DEVELOPMENT

## Slide 16: METHODOLOGY
Competitive Product Analysis
Brain Storming
Taking Advantage of Known Characteristics of Glass Nanoparticles

## Slide 17: Typical Construction Process
  Cover
    Thick sheets of cardboard paper
  Special Gypsum Plaster
    Gypsum
    Soap
    Nano Glass Particles
    Water
Thick Sheet of Paper
Gypsum Plaster
It’s a panel made of gypsum plaster pressed between two thick sheets of paper.

## Slide 18: Typical Construction Process

## Slide 19: Engineering Challenge
How to make equivalent sheets of drywalls using standard materials & Proposed Next Generation drywalls of varying compositions using different amounts of glass nanoparticles?
Develop reproducible samples by designing your own mold!

## Slide 20: Functional Decomposition

## Slide 21: Functional Decomposition for Next Generation Drywall
Mold
Gypsum Plaster
Testing

## Slide 22: Sub Function I Mold
Design Constraints |  | 
Cost |  | 
Heat Resistant |  | 
Manufacturability |  | 
Concept Variants |  | 
Steel |  | 
Aluminum |  | 
Plastic |  | 
Mold | Cost | Heat Resistant | Manufacturability | Row Sum | Nominal Score (Rel. Weight)
Cost |  | 2 | 2 | 4 | 0.222
Heat Resistant | 4 |  | 5 | 9 | 0.500
Manufacturability | 4 | 1 |  | 5 | 0.278
Col. Sum | 8 | 3 | 7 | 18 | 1.000

## Slide 23: Sub Function I Mold
COST (min) | Steel | Aluminum | Plastic | Row Sum | Nominal Score (Rel. Weight)
Steel |  | 2 | 1 | 3 | 0.167
Aluminum | 4 |  | 2 | 6 | 0.333
Plastic | 5 | 4 |  | 9 | 0.500
Col. Sum | 9 | 6 | 3 | 18 | 1.000
Heat Resistant > 450° C | Steel | Aluminum | Plastic | Row Sum | Nominal Score (Rel. Weight)
Steel |  | 4 | 5 | 9 | 0.500
Aluminum | 2 |  | 5 | 7 | 0.389
Plastic | 1 | 1 |  | 2 | 0.111
Col. Sum | 3 | 5 | 10 | 18 | 1.000
Manufacturability | Steel | Aluminum | Plastic | Row Sum | Nominal Score (Rel. Weight)
Steel |  | 2 | 2 | 4 | 0.222
Aluminum | 4 |  | 5 | 9 | 0.500
Plastic | 4 | 1 |  | 5 | 0.278
Col. Sum | 8 | 3 | 7 | 18 | 1.000
 | Cost | Heat Resitant | Manufacturability | SCORE
Steel | 0.037 | 0.250 | 0.062 | 0.349
Aluminum | 0.074 | 0.194 | 0.139 | 0.407
Plastic | 0.111 | 0.056 | 0.077 | 0.244

## Slide 24: Sub Function II Special Gypsum Plaster
Gypsum
Soap
Nano Glass Particles
Special Gypsum Plaster
Design Constraints |  | 
Strength |  | 
Fire Resistant |  | 
Weight |  | 
Concept Variants |  | 
Type of Gypsum |  | 
Nano Glass Particle Reinforcement |  | 
Process Time |  | 
Gypsum Plaster | Strength | Fire Resistant | Weight | Row Sum | Nominal Score (Rel. Weight)
Strength |  | 1 | 4 | 5 | 0.278
Fire Resistant | 5 |  | 5 | 10 | 0.556
Weight | 2 | 1 |  | 3 | 0.167
Col. Sum | 7 | 2 | 9 | 18 | 1.000

## Slide 25: Sub Function II Special Gypsum Plaster
Gypsum
Soap
Nano Glass Particles
Special Gypsum Plaster
Strength | Type 0f Gypsum | Nano Glass Particle Reinforcement | Process Time | Row Sum | Nominal Score (Rel. Weight)
Gypsum |  | 2 | 4 | 6 | 0.333
Nano Glass Particles | 4 |  | 4 | 8 | 0.444
Process Time | 2 | 2 |  | 4 | 0.222
Col. Sum | 6 | 4 | 8 | 18 | 1.000
Fire Resistant | Type 0f Gypsum | Nano Glass Particle Reinforcement | Process Time | Row Sum | Nominal Score (Rel. Weight)
Gypsum |  | 1 | 4 | 5 | 0.278
Nano Glass Particles | 5 |  | 6 | 11 | 0.611
Process Time | 2 | 0 |  | 2 | 0.111
Col. Sum | 7 | 1 | 10 | 18 | 1.000
Weight (Min) | Type 0f Gypsum | Nano Glass Particle Reinforcement | Process Time | Row Sum | Nominal Score (Rel. Weight)
Gypsum |  | 4 | 2 | 6 | 0.333
Nano Glass Particles | 2 |  | 2 | 4 | 0.222
Process Time | 4 | 4 |  | 8 | 0.444
Col. Sum | 6 | 8 | 4 | 18 | 1.000
 | Strength | Fire Resistant | Weight | Score
Type of Gypsum | 0.093 | 0.154 | 0.056 | 0.302
Nano Glass Particle Reinforcement | 0.123 | 0.340 | 0.037 | 0.500
Process Time | 0.062 | 0.062 | 0.074 | 0.198
 |  |  |  | 1.000

## Slide 26: Sub Function III Testing
Design Constraints |  | 
R-Value |  | 
ASTM 1396 |  | 
ASTM 119 |  | 
Concept Variants |  | 
Volume |  | 
% Nano Particles |  | 
Temperature |  | 
Testing | R-Value | STC 57 | ASTM E119 TEST | Row Sum | Nominal Score (Rel. Weight)
R-Value |  | 4 | 3 | 7 | 0.389
ASTM 1396 | 2 |  | 1 | 3 | 0.167
ASTM E119 TEST | 3 | 5 |  | 8 | 0.444
Col. Sum | 5 | 9 | 4 | 18 | 1.000

## Slide 27: Sub Function III Testing
R-Value | Volume | % Nano Particles | Temperature | Row Sum | Nominal Score (Rel. Weight)
Volume |  | 2 | 1 | 3 | 0.167
% Nano Particles | 4 |  | 4 | 8 | 0.444
Temperature | 5 | 2 |  | 7 | 0.389
Col. Sum | 9 | 4 | 5 | 18 | 1.000
ASTM 1396 | Volume | % Nano Particles | Temperature | Row Sum | Nominal Score (Rel. Weight)
Volume |  | 4 | 6 | 10 | 0.556
% Nano Particles | 2 |  | 5 | 7 | 0.389
Temperature | 0 | 1 |  | 1 | 0.056
Col. Sum | 2 | 5 | 11 | 18 | 1.000
ASTM E119 TEST | Volume | % Nano Particles | Temperature | Row Sum | Nominal Score (Rel. Weight)
Volume |  | 2 | 3 | 5 | 0.278
% Nano Particles | 4 |  | 4 | 8 | 0.444
Temperature | 3 | 2 |  | 5 | 0.278
Col. Sum | 7 | 4 | 7 | 18 | 1.000
 | R-Value | ASTM 1396 | ASTM E119 TEST | Score
Volume | 0.0648 | 0.0925 | 0.123 | 0.281
% Nano Particles | 0.172 | 0.06481 | 0.198 | 0.435
Temperature | 0.15123 | 0.00925 | 0.123 | 0.284

## Slide 28: Gypsum Drywall Type X
Special fire-resistance
It provides a greater fire-resistance than regular gypsum board of the same thickness
When tested with the Test Methods E119, shall provide a minimum fire resistance of:
  For 5/8” thickness: one hour
  For ½” thickness: two hours

## Slide 29: Product Concept
  Mold
    Body (10” X 10” X 1”)
    Lid for 1/2” & 5/8” thickness
½” (13 mm)
5/8”
(16 mm)

## Slide 30: Product Concept (Continued)
Use mold to develop identical samples for comparison
Use various percent of glass nanoparticles
Use similar process conditions to make samples
ASTM E 119-00a standard test specification will need to be adjusted

## Slide 31: DESIGN EMBODIMENT

## Slide 32: Engineering Challenges
Not standardized sample may result in high variance data.
Fire resistant test temperature not constant
ASTM E 119-00a standard test specification will need to be adjusted
Acoustic tests need be developed using University resources

## Slide 33: Engineering Analysis
Thermal conductivity
Samples with 0%, 10%, 20% and 30% Glass nanoparticles tested

## Slide 34: Engineering Analysis
Thermal conductivity
Gypsum board walls
Bottom polystyrene
Plate to hold light blobs
Inside temperature
Known, outside
Temperature measure,
3 thermocouples

## Slide 35: Engineering Analysis
International Standard ISO 140/3
Sound Reduction index
Samples with 0%, 10%, 20% and 30% Glass nanoparticles tested

## Slide 36: Preliminary/Supportive Experiments
Fire Endurance test
Follows E119 ASTM standard operations
Fixed load applied to sample up to failure
Constant monitoring of temperature, 5 min intervals
Results will be plug into the Time/Temp. graph
5/8’’

## Slide 37: Preliminary/Supportive Experiments
Sound Reduction Index
Box created with sample drywall will be measure for acoustic reduction
Digital sound lever meter use to read the sound pressure
Experiments will be done at specific frequencies AND typical mix as in a music
Results will estimate the sound reduction index at various frequencies and typical noise/music environment

## Slide 38: Proposed Product
Gypsum drywall sample
Measurements:
  10” x 10” x 5/8”
  10” x 10” x ½”
Percentage of Glass nanoparticles
0% -control group
10%, 20%, 30%
10 in
10 in

## Slide 39: Design for Manufacturability
Scale Mold Prototype
  Mold drawings
10 ft by 10 ft Drywall
  5/8’’ thickness

## Slide 40: Manufacturing Process Operation Process Chart
0101
Gypsum Preparation
Heating, Mixing, Cooling, Inspect
0102
Chemicals Mixing
Chemical Treatment, Mixing, Inspect
Molding
0103
Heating, Paper layers, Cooling, Inspect
SA1
A1
I1
3001
3050
3002
Nano Glass Particles
Soap
Gypsum

## Slide 41: Manufacturing Process Precedence Diagram
0100
0103
A1
SA1
0102
0101
I1
3001
3002
3050

## Slide 42: DESIGN VALIDATION

## Slide 43: Bill of Materials / Drywall
No Cost

## Slide 44: Economic Analysis
Prototype cost of production items

## Slide 45: Economic Analysis
Target cost: less than $12.00 dlls.
Retail cost: $10.97 dlls.
Competitive Cost : $10.00 - $12.00 dlls.
Prototype production cost:
  $97.15 dlls for 12 plates of 5/8” x 12” x 12”

## Slide 46: Test Protocols
Test ID | Test Description | Expected Results | Actual Results
E 119 | Fire Resistance | >= to 1 Hour | 
E 84 | Flame Retardant | Index <= than 25 | 
C 473 Method A | Hardness | >= than 15 lbf [67 N] | 
C 473 Method B |  | >= than 11 lbf [49 N] | 
C 473 Method A (Perpendicular) | Flexural Strength | >= than 150 lbf [667 N] | 
Method A (Parallel) |  | >= than 50 lbf [222 N] | 
C 473 Method B (Perpendicular) |  | >= than 147 lbf [654 N] | 
C 473 Method B (Parallel) |  | >= than 46 lbf [250 N] | 
C 1396 | Humidified Deflection | <= than 5 eighths of an inch [16 mm] | 
C 473 Method A | Nail Pull Resistance | >= than 90 lbf [400 N] | 
C 473 Method B |  | >= than 87 lbf [387 N] | 
For a 5/8’’ thickness drywall

## Slide 47: FMEA / Mold
FAILURE MODE AND EFFECTS ANALYSIS FOR MOLD |  |  |  |  |  |  | 
Process Function | Potential Failure Mode | Severity | Potential Cause(s)/ Mechanism(s) of Failure | Frequency | Current Process Controls | Ability to Detect | RPN
Form and shape drywall | Failure to resist high temperatures | 8 | Improper machine set up | 2 | Operator training and instructions | 6 | 96
 | Breaks | 9 | Improper machine set up | 4 | Operator training and instructions | 8 | 288

## Slide 48: FMEA / Drywall
FAILURE MODE AND EFFECTS ANALYSIS FOR DRYWALL |  |  |  |  |  |  | 
Process Function | Potential Failure Mode | Severity | Potential Cause(s)/ Mechanism(s) of Failure | Frequency | Current Process Controls | Ability to Detect | RPN
Construction Support, Fire Resistance, lower vibration transmission | Not enough fire resistivity | 9 | Not proper gypsum mixing | 4 | Standards Instructions how to prepare gypsum mix | 6 | 216
 | Low soundproof index | 4 | Improper gypsum mixing and not proper thickness | 5 | Standards Instructions how to prepare gypsum mix | 3 | 60
 | Low Humidity | 7 | Not proper gypsum mixing | 5 | Standards Instructions how to prepare gypsum mix | 3 | 105

## Slide 49: Safety analysis
Fine nanopowders are safely handled using appropriate gloves & masks

## Slide 50: Selected Safety Information for Glass Micro & Nano Particles
Acute Toxicity: None known
Chronic Toxicity: None known
Causes Eye Irritation
May Cause Respiratory Irritation
Avoid Breathing Dust
Wear Personal Protective Equipment (PPE)
Source: MSDS#031512 (Precision Recycling Industries, Cornelius, NC (Revised 03/20/2012

## Slide 51: SUMMARY
Identified a new opportunity to build next generation drywalls using glass micro- & nano-particles from recycled glass.
Expected benefits include environment friendly fire resistant materials, more energy savings, & better noise attenuation
Developed reproducible sample drywalls using standard & proposed new drywalls with varying percent of glass nanoparticles
Will use standard test protocols for fire resistance and insulation
Will develop new protocols for noise attenuation using University resources

## Slide 52
Gantt Chart
Next Generation Drywall |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  |  |  |  |  |  |  | Plan |  |  | Actual |  |  |  | Complete | 
ACTIVITY | PERIODS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | 5-Sep | 12-Sep | 19-Sep | 26-Sep | 3-Oct | 6-Oct | 10-Oct | 17-Oct | 24-Oct | 27-Oct | 31-Oct | 7-Nov | 10-Nov | 14-Nov | 17-Nov | 21-Nov | 1-Dec | 5-Dec
Problem Formulation |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Elevator Speech |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Background Research |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Competitive products |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Needs and Wants |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Goals, Objectives & Constraints |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Group presentation 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
QFD |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Group presentation 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Mold - Buy Aluminum |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Concept generation |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Functional Decomposition |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Methodology for Concept Development |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Concept Generation |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Concept Selection |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Product Concept |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Group Presentation 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Mold Making (Milling) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Design Embodiment |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Product Drawings |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Engineering Challenges/Topics |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Engineering Analysis: Tables & Graphs |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Preliminary/Supportive experiments |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
proposed Product |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
BOM |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Group Presentation 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Design Validation |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Test Protocols |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Design for Manufacturability |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Manufacturing Process |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
DFMEA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
QA Protocols for Parts & Assembly |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Design History file (DHF) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Final Report Due |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Final Group Presentetaion |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 53: References
www.globalgypsum.com
www.buildgp.com
www.nationalgypsum.com/about/index.htm
www.USG.com
www.Continental-bp.com
www.lowes.com
www.Homedepot.com

## Slide 54: Questions?
Thank you!